# SECTION 097200

DIGITALLY PRINTED VINYL WALLCOVERING MURALS

PART 1 - GENERAL

  - SUMMARY

    - Provide digitally printed wallcovering vinyl wallcovering, complete.

    - Related Sections

      - Section 16500 - Lighting: Permanent during installation.

      - Section 09250 - Gypsum Board: Wall Substrates.

      - Section 09900 - Painting: Preparation and priming of substrate surfaces.

  - REFERENCES

    - American Society for Testing and Materials (ASTM):

      - E 84	Test Method for Surface Burning Characteristics of Building Materials.

    - Wallcovering Association (WA):

      - WA-101-2011	Quality Standard for Polymer Coated Fabric Wallcovering.

    - Federal Specifications (FedSpec):

2.	CCC-W- 408A	Wallcovering, Vinyl Coated

    - Underwriters Laboratory, Inc. (UL)

      - UL 723:	Test for Surface Burning Characteristics of Building Materials

- National Fire Protection Agency (NFPA)

  - NFPA 101	Life Safety Code

  - NFPA 286	Standard Methods of Fire Tests for Evaluating Contribution of Wall

and Ceiling Interior Finish to Room Fire Growth

  - CAN/ULC-S102	Test for Surface Burning Characteristics of Building Materials and

Assemblies

  - SUBMITTALS

    - Submit one Color Proof for approval prior to manufacture of a full size miniature mural.

    - Submit one full size miniature strike-off for approval prior to the manufacture of full size mural.

    - Submit manufacturers' product data and installation instructions for each digitally printed wallcovering mural, adhesive and accessory required.

      - Include data on physical properties, fire hazard classification and fire detection characteristics of wallcovering.

      - Include manufacturer's recommendations for maximum permissible moisture content of substrates.

    - Submit full-size samples, 54 inches wide by 36 inches long, cut from current production of each ground wallcovering selected to demonstrate quality, weight, color and embossing.

    - Submit manufacturer's written product certification that all furnished wallcovering ground meets or exceeds the specification requirements. Include certified copies of tests specified.

    - Submit wallcovering ground manufacturer's written instructions for recommended maintenance of each type of wallcovering required.

  - QUALITY ASSURANCE

    - Manufacturer: Provide each type of digitally printed vinyl wallcovering mural required produced by one manufacturer whose published product literature clearly indicates compliance of wallcovering ground with specified requirements.

    - Applicator: Installation by skilled commercial wallcovering applicators with no less than three years of documented experience installing wallcovering murals of the types and extent specified for the project.

    - Material Standards: Provide materials that meet or exceed Federal Specification CCC-W-408A and WA- 101 Quality Standard for Polymer Coated Fabric Wallcovering for Type I and Type II wallcovering.

    - Physical Properties: Provide wallcovering with the following physical properties when tested in accordance with ASTM D751.

      - Total weight:	21 oz./lin. yd

      - Tensile Strength:	50 X 55 Minimum (W x F)

      - Tear Strength:	25 X 25 Minimum (W x F)

    - Fire Hazard Classification: Provide materials that comply with Class A fire rating when tested in accordance with ASTM E84.

    - Underwriters Laboratories approval: Provide materials that have been tested and approved by Underwriters Laboratories.

    - Smoke Toxicity: Provide materials that have been tested for smoke toxicity and approved for use by New York City Materials and Equipment Acceptance Division (MEA).

    - Fire Detection Characteristics: Provide materials that have been laboratory tested for the Early Warning Effect® in accordance with ASTM E 603. Submit test results certifying that when one square foot section of the material is heated to 300 degrees F, the wallcovering emits an odorless, colorless non-toxic vapor that will activate an ionization smoke detector.

    - Low Emissions: Provide materials that meet the requirements of California Integrated Waste Management Board’s Special Environmental Requirements Specification CA 01350 for low emitting materials.

  - PRODUCT DELIVERY, STORAGE AND HANDLING

    - Deliver digitally printed vinyl wallcovering mural to the project site in unbroken and undamaged wrappings and clearly labeled with the manufacturer's identification label, quality or grade, UL label and sidemark.

    - Store materials in a clean, dry storage area with temperature maintained above 55 degrees with normal humidity.

    - Store material in a flat position to prevent damage to roll-ends. Do not cross stack material. Support material off the floor in a manner to prevent sagging and warping.

  - PROJECT CONDITIONS

    - Do not apply digitally printed wallcovering mural when surface and ambient temperatures are outside the temperature ranges required by the wallcovering manufacturer.

    - Provide continuous ventilation and heating facilities to maintain substrate surface and ambient temperatures above 60 degrees F unless required otherwise by manufacturer's instructions.

    - Apply adhesive only when substrate surface temperature or ambient temperature is above 60 degrees F, or relative humidity is below 40 percent.

    - Maintain constant recommended temperature and humidity for at least 72 hours prior to, throughout the installation period and for 72 hours after wallcovering installation completion.

    - Provide not less than an 80 foot candles per square foot lighting level minimum measured mid height at substrate surfaces.

  - WARRANTY

    - Submit manufacturer’s 5 year written warranty against manufacturing defects.

# PART 2 - PRODUCTS

  - MANUFACTURERS

    - Digitally Printed Wallcovering Mural: Koroseal Digitally Printed Wallcovering Murals manufactured by Koroseal Interior Products, LLC.  Contact sales representative 	.

  - MATERIALS

    - Wallcovering:  Koroseal Digital Surfaces Wallcovering , Pattern: 	. Type II conforming to Federal Specification CCC-W-408A and WA-101-A using test methods given in Federal Specification CCC-T-191 b excepted as otherwise specified.

      - Total Weight:	21 ounces per linear yard.

      - Backing Weight:	3.1 ounces per linear yard.

      - Vinyl Weight:	17.9 ounces per linear yard

      - Thickness:	0.018 to 0.026 inches

      - Fabric backing and content:	Poly-Cotton Woven

    - Digital Image: Owner/Architect to provide PDF file of image to be digitally printed with UV inks on Koroseal Digital Surfaces Type II Wallcovering

  - ACCESSORIES

    - Adhesives: Koroseal A-848-B Heavy-Duty Premixed vinyl adhesive.

    - Substrate Primer/Sealer: White pigmented alkyd or acrylic/latex base primer specifically formulated for use with vinyl wallcoverings.

    - [Optional] Metal Moldings: Extruded aluminum, alloy 6063-T5, long lengths, with fine satin mechanical finish and class 2 clear architectural anodic coating conforming to AA M21A31 designed for use with vinyl wallcoverings.

# PART 3 - EXECUTION

  - EXAMINATION

    - Examine substrates and installation conditions.

- Test substrates with a suitable moisture meter and verify that moisture content does not exceed 4 percent

- Verify substrate surfaces are clean, dry, smooth, structurally sound and free from surface defects and imperfections that would show through the finished surface.

- Evaluate all painted surfaces for the possibility of pigment bleed-through.

- Notify the contractor and architect in writing of any conditions detrimental to the proper and timely completion of the installation. Beginning of installation means acceptance of surface conditions.

  - INSTALLATION

    - Allow digitally printed vinyl wallcovering mural to acclimatize to the area of installation a minimum of 24 hours before installation.

    - Before cutting, examine image and color and determine that they are the correct image and color as specified for the correct location.

    - Read and follow the instructions in the manufacturer's installation sheet contained in each roll of the digitally printed vinyl wallcovering mural.

    - Use adhesive recommended by the wallcovering manufacturer.

    - Install each panel in sequence as indicated on the drawings.

    - If there are variations in color or image that are considered to be excessive, notify the manufacturer's representative for an inspection before any further wallcovering is installed.

    - Smooth wallcovering to the hanging surface using a stiff bristled sweep brush to eliminate air bubbles, wrinkles, gaps and overlaps.

    - Remove excess adhesive along finished seams immediately after each wallcovering strip applied. Use clean warm water, a natural sponge and clean towels. Change water often to maintain water cleanliness.

  - CLEAN-UP COMPLETION

    - Upon completion of the work, remove surplus materials, rubbish and debris resulting from the wallcovering installation. Leave areas in neat clean and orderly condition.

END OF SECTION